## Slide 1
University of Minho School of Engineering 3B’s Research Group | 
Uma Escola a Reinventar o Futuro – Semana da Escola de Engenharia - 24 a 27 de Outubro de 2011
Engineering Osteochondral Tissue
CRISTINA CORREIA*
Supervisors: Rui L. Reis, Rui A. Sousa, Gordana Vunjak-Novakovic
* ccorreia@dep.uminho.pt
ENGINEERING OSTEOCHONDRAL TISSUE BY HUMAN ADIPOSE STEM CELLS USING BIOMECHANICAL AND BIOCHEMICAL STIMULI
Human Adipose Stem Cell (hASC) isolation, characterization and multi-lineage differentiation potential
Engineering Bone Tissue
hASC stimulation with Pulsatile Fluid Flow
400 µm/sec
1200 µm/sec
A
B
C
Material: Gellan gum hydrogel
suitable matrix and mechanical properties1
Stimuli: Hydrostatic pressure
major force acting in vivo on articular cartilage2
Material: Silk fibroin sponge
adequate structure and mechanical properties3
Stimuli: Shear stress
major force detected by bone cells in vivo4
Material: Fibrin hydrogel
angiogenic properties5
Stimuli: Growth factors
temporal nourishment with angiogenic growth factors6
Vascularizing Engineered Bone
hASC stimulation with temporal growth factor (GF) nourishment
Engineering Cartilage Tissue
hASC stimulation with Pulsatile Hydrostatic Pressure
Pre-differentiation of hASC at continuous fluid flow, before application of pulsatile fluid flow increased bone tissue development
In order to develop both tissues, a sequential induction of cells and GF was critical. Osteogenic induction should precede vasculogenesis.
Enzymatic digestion of lipoaspirate
hASC isolation and expansion
Characterization of cell surface markers by flow cytometry
Chondrogenic (B), Adipogenic (C), and Osteogenic (D) differentiation
Hydrostatic pressure culture of hASC for 4 weeks increased aggrecan (cartilage protein) gene expression relatively to static culture (p<0.001)
Acknowledgments: Sarindr Bhumiratana, Warren Grayson, Rita Duarte, Adriano Pedro, Luisa Pereira, for technical support; Portuguese Foundation for Science and Technology for PhD grant SFRH/BD/42316/2007.
References: 1Oliveira JT et al, JBMR (2009), 2Hu JC et al, TE (2006); 3Kim UJ et al , Biomat (2005); 4Weinbaum et al , J Biomech (1994); 5Dvorak HF et al, Lab Invest (1987); 6Correia C et al (subm.)
Columbia University
Bone proteins
Mineral
Vascular proteins
Bone proteins
Immunolocalization
B
A
C
D
A) HP vessel assembly;
B) Schematic representation of HP bioreactor;
C) Direction of forces applied to construct during stimulation;
D) Photograph of HP bioreactor
Pressure | Frequency | Duration
50 Bar | 0.5 Hz | 4h/day
Conclusions
The adoption of a holistic approach concerning the single use of hASCs for the full engineering of osteochondral tissues proved successful. In this regard, the combined application of dynamic culturing conditions, namely of hydrostatic pressure and fluid flow, with biochemical cues, such as chondrogenic, osteogenic and angiogenic growth factors can be integrated in the manufacturing of osteochondral grafts.